Product Type:  NYLON CARPET TILE

Title: IDL CANTERBURY

Description: IDL CANTERBURY reflects the timeless design inspired by Roman roots, blending heritage with contemporary refinement. Its structured texture echoes the architectural character found in historic cities like Ely and Exeter. Crafted for modern commercial spaces, Canterbury delivers a classic yet confident aesthetic that brings depth, order, and enduring style to interiors.

Code: IDL CANTERBURY 01, 02,03,04,06

Colors: 5

Applications: HIGH TRAFFIC COMMERCIAL SPACES

Sustainability:

Technical Specs:

| IDL CANTERBURY |  |
| --- | --- |
| PARAMETER | SPECIFICATIONS |
| CONSTRUCTION | MULTI-LEVEL LOOP-NEEDLE BAR SHIFT |
| YARN | 100% UNIVERSAL (USA)-PRESTIVA*NYLON 6 |
| COLOUR SYSTEM | 100% SOLUTION DYED |
| STITCHES & GAUGE | 1/12 |
| TOTAL TUFTED PILE WEIGHT | 540 GSM (16 Oz/Yd²) |
| TOTAL WEIGHT | 4200 gm/m² (+/- 100gm) |
| PRIMARY BACKING | NON-WOVEN |
| SECONDARY BACKING | HIGH PERFORMANCE PVC REINFORCED WTH FIBERGLASS |
| TILE SIZE | 25cm X 100cm |
| PACKING | 20 TILES/BOX (5.00 SQM) |

Performance Ratings:

| PERFORMANCE RATING |  |
| --- | --- |
| AREA OF USE | CLASS 33-HEAVY COMMERCIAL |
| FIRE CLASS | ASTM D2859-16 |
| FORMALDEHYDE | CRI CERTIFIED |
| DIMENSIONAL STABILITY | ASTM D7570 |
| ELECTROSTATIC PROPENSITY | AATCC 134-2019 |

Ideal Applications: